DANTEc Materials Science Repository – Activity Taxonomy

| Activity | Subclass | Feature | Parameters | Methods/techniques |
| --- | --- | --- | --- | --- |
| Structure analysis | Atomic & Molecular structure | Elementary composition | Elementary composition (relative or absolute) | XRF (X-ray fluorescence), ICP-MS (Inductively couples plasma – mass spectrometry), AAS (atomic absorption spectroscopy),OES (optical emission spectroscopy), EDS (energy-dispersive X-ray spectroscopy) |
|  |  | Crystal structure | Lattice parameters; space group; crystallinity; phase fraction | XRD (X-ray diffraction); neutron/electron diffraction; DSC (differential scanning calorimetry) |
|  |  | Atomic bonding & coordination | Coordination number; bonding type; oxidation state | XAS (X-ray absorption spectroscopy; EXAFS/XANES); Raman spectroscopy; FTIR (Fourier-transform infrared spectroscopy); XPS/ESCA (X-ray photoelectron spectroscopy); UPS (UV photoelectron spectroscopy) |
|  |  | Point defect structure | Vacancy/interstitial concentration; site occupancy; lattice distortion | PAS (positron annihilation spectroscopy); APT (atom probe tomography); TEM (transmission electron microscopy); Mössbauer spectroscopy |
|  | Microstructure | Grain architecture | Mean grain size; size distribution; aspect ratio; morphology | Optical microscopy; SEM (scanning electron microscopy); EBSD (electron backscatter diffraction) |
|  |  | Grain boundary character | Misorientation angle; boundary type; Σ-values | EBSD (electron backscatter diffraction); TEM (transmission electron microscopy); STEM (scanning transmission electron microscopy) |
|  |  | Phase distribution & morphology | Phase fraction; connectivity; precipitate size/density | SEM (scanning electron microscopy) with EDS (energy-dispersive X-ray spectroscopy); XRD (X-ray diffraction); APT (atom probe tomography); SAXS/WAXS (small-/wide-angle X-ray scattering) |
|  |  | Porosity & void analysis | Pore size distribution; volume fraction; connectivity | XCT (X-ray computed tomography); SEM (scanning electron microscopy); BET (gas adsorption, Brunauer–Emmett–Teller); MIP (mercury intrusion porosimetry) |
|  |  | Crystallographic texture | Preferred orientation; ODF (orientation distribution function); pole figures | EBSD (electron backscatter diffraction); XRD (X-ray diffraction); neutron diffraction |
|  |  | Interface & interphase character | Interface thickness; roughness; chemistry; adhesion indicators | SEM (scanning electron microscopy); TEM (transmission electron microscopy); XPS (X-ray photoelectron spectroscopy); XRR (X-ray reflectivity) |
|  | Macrostructure | Layered & coating geometry | Layer thickness; sequence; continuity; uniformity | Profilometry; SEM (scanning electron microscopy, cross-section); XCT (X-ray computed tomography); ellipsometry |
|  |  | Macro-scale homogeneity | Segregation patterns; density gradients; compositional gradients | Macro-etching; X-ray radiography; XCT (X-ray computed tomography); ultrasonic testing (NDT) |
|  |  | Damage & defect mapping | Crack length/depth; delamination area; defect location; integrity | Visual inspection; NDT (ultrasonic testing, eddy-current testing); X-ray radiography; XCT (X-ray computed tomography) |
|  |  | Joint & assembly geometry | Weld bead geometry; HAZ (heat-affected zone) extent; fusion zone width | Optical microscopy; SEM (scanning electron microscopy); X-ray radiography; ultrasonic testing (NDT) |
| Property analysis | Mechanical Properties | Quasi-static strength | Yield strength; UTS (ultimate tensile strength); proof stress; stress–strain curve | Uniaxial tensile/compression/shear testing (UTM/servo-hydraulic test frames) |
|  |  | Elasticity & stiffness | E/G/K moduli; Poisson’s ratio | Tensile testing; resonance frequency analysis; nanoindentation |
|  |  | Plasticity & ductility | Elongation at break; reduction of area; strain hardening | Tensile/bend testing; DIC (digital image correlation) |
|  |  | Hardness | HV/HB/HR; nanohardness | Indentation testing; nanoindentation |
|  |  | Fracture & toughness | KIC; impact energy; DBTT (ductile-to-brittle transition temperature) | Fracture mechanics testing; Charpy/Izod impact testing |
|  |  | Fatigue & cyclic behavior | S–N response; endurance limit; da/dN | Fatigue testing (HCF/LCF); rotating-bending fatigue |
|  |  | Creep & relaxation | Creep rate; time to rupture; stress relaxation rate | Creep testing (furnace); constant-load testing; Rheology |
|  | Electrical & Electronic | Charge transport | Conductivity; resistivity; carrier mobility/concentration | Four-point probe; Hall effect; impedance spectroscopy |
|  |  | Dielectric & ferroelectric | Dielectric constant (εr); loss tangent (tan δ); breakdown strength | LCR meter; impedance spectroscopy |
|  |  | Semiconducting behavior | Band gap; carrier type; recombination lifetime | UV–Vis spectroscopy; photoluminescence (PL); Hall effect |
|  |  | Superconductivity | Tc; Ic; Hc | SQUID (superconducting quantum interference device) magnetometry; transport measurements |
|  | Thermal Properties | Thermal transport | Thermal conductivity; thermal diffusivity | LFA (laser flash analysis); 3-omega method |
|  |  | Calorimetry | Cp; enthalpy of transition (ΔH) | DSC (differential scanning calorimetry); adiabatic calorimetry |
|  |  | Thermal expansion | CTE; thermal strain; anisotropy | Dilatometry; TMA (thermomechanical analysis); high-temperature XRD (X-ray diffraction) |
|  |  | Thermal stability | Decomposition temperature; mass loss (%) | TGA (thermogravimetric analysis); TGA-DSC; in-situ XRD (X-ray diffraction) |
|  | Thermoelectric | Thermoelectric transport | Seebeck coefficient; Peltier/Thomson coefficients | Seebeck measurement; Peltier characterization |
|  |  | Thermoelectric efficiency | ZT; power factor (S²σ) | Integrated ZT measurement systems |
|  | Magnetic Properties | Magnetization | Susceptibility; Ms; Mr | SQUID (superconducting quantum interference device); VSM (vibrating sample magnetometry); magnetic balance |
|  |  | Magnetic switching | Coercivity (Hc); loop area; squareness ratio | VSM (vibrating sample magnetometry); SQUID (superconducting quantum interference device); MFM (magnetic force microscopy) |
|  |  | Magneto-transport | Magnetoresistance (GMR/TMR/AMR); Hall effect | Cryogenic transport; four-point probe in magnetic field |
|  |  | Magnetocaloric effect | ΔTad; ΔSM | Direct calorimetry; SQUID (superconducting quantum interference device) |
|  | Optical Properties | Photonic response | Absorption coefficient; reflectance; refractive index | UV–Vis–NIR spectroscopy; ellipsometry; prism coupling |
|  |  | Luminescence | Emission wavelength; quantum yield; lifetime | Photoluminescence (PL); fluorescence spectroscopy |
|  |  | Vibrational spectroscopy | Raman shift; phonon modes; disorder parameter | Raman spectroscopy; FTIR (Fourier-transform infrared spectroscopy) |
|  | Surface & Interfacial | Surface energy & wetting | Contact angle; surface energy; work of adhesion | Sessile-drop goniometry; AFM (atomic force microscopy) |
|  |  | Interfacial adhesion | Adhesion strength; pull-off force; shear strength | Scratch testing; peel testing; nanoindentation |
|  |  | Biocompatibility | Cell viability; proliferation; protein adsorption | Cell culture assays; MTT assay; immunofluorescence microscopy |
|  | Tribological Properties | Friction & lubrication | Coefficient of friction; lubrication film thickness | Tribometry (pin-on-disk/ball-on-disk); optical interferometry |
|  |  | Wear resistance | Wear volume/rate; debris morphology | Abrasive wear testing; tribometry; SEM (scanning electron microscopy) |
|  |  | Surface topography | Ra/Rz; asperity distribution | Profilometry; AFM (atomic force microscopy); confocal microscopy |
|  | Chemical & Electrochemical | Corrosion & oxidation | Corrosion rate; Ecorr; oxidation kinetics | Potentiodynamic polarization; salt spray testing; TGA (thermogravimetric analysis), OCP (open circuit potential) |
|  |  | Catalytic activity | TOF/TON; conversion; selectivity | Catalytic reactor testing; GC/MS (gas chromatography–mass spectrometry); in-situ spectroscopy |
|  |  | Mass transport | Diffusion coefficient; permeability; flux | SIMS (secondary ion mass spectrometry); tracer diffusion; gas permeation testing |
|  |  | Electrochemical storage | Specific capacity; Coulombic efficiency; charge/discharge curves | Galvanostatic cycling; potentiostatic testing; battery cycling |
|  |  | Electrochemical kinetics | Overpotential; i0; Tafel slope | CV (cyclic voltammetry); LSV (linear sweep voltammetry); EIS (electrochemical impedance spectroscopy); Tafel analysis |
|  |  | Ionic transport | Ionic conductivity; transference number; activation energy | EIS (electrochemical impedance spectroscopy); conductivity cell; potentiostatic/galvanostatic testing |
|  | Acoustic & Vibrational | Acoustic propagation | Wave velocities; acoustic impedance; attenuation | Ultrasonic testing; acoustic microscopy; resonance frequency analysis; Brillouin scattering |
|  |  | Damping & absorption | Sound absorption coefficient; loss tangent; damping ratio; Q factor | Impedance tube; DMA (dynamic mechanical analysis); reverberation room method |
|  |  | Lattice dynamics | Phonon dispersion/DOS; Debye temperature | INS (inelastic neutron scattering); Raman spectroscopy; Brillouin scattering; DFT (density functional theory) |
|  | Extreme Environments | Radiation damage | dpa; swelling; hardness change; embrittlement indicators | Ion/neutron irradiation; PIE (post-irradiation examination); nanoindentation |
|  |  | Thermal shock | Strength retention; fracture after cycling | Rapid thermal cycling; mechanical testing post-cycling |
|  |  | Cryogenic performance | Low-temperature strength; ductility; impact energy | Cryogenic tensile/impact testing |
| Performance evaluation | Service performance | Operational stability | Signal-to-noise ratio; efficiency under load; drift rate | Long-term stability logging; operando/in-situ test rigs |
|  |  | Combined loading | Synergistic degradation; SCC index; creep–fatigue interaction | Multi-axial testing; environmental fatigue rigs; TMF (thermo-mechanical fatigue) |
|  | Durability & Lifetime | Accelerated aging | Degradation factor; acceleration shift factor; Arrhenius activation energy | Salt spray (ASTM B117); QUV (UV weathering); HAST (highly accelerated stress test); climatic chamber testing |
|  |  | Reliability & failure | Weibull modulus; MTTF; B10 life | Step-stress testing; statistical reliability modeling |
|  |  | Wear & erosion life | Material loss rate vs time; breakthrough time | Long-term tribo-testing; sand/slurry erosion testing; field exposure |
|  | Damage Tolerance | Failure mode analysis | Fracture surface morphology; crack path; initiation site | Fractography (SEM—scanning electron microscopy); cross-sectional analysis; failure mapping |
|  |  | Defect sensitivity | Critical flaw size; notch sensitivity; CAI (compression after impact) | Fracture mechanics testing; NDE (non-destructive evaluation) correlation |
| Processing & fabrication | Feedstock & Synthesis | Precursor preparation | Particle size; morphology; purity; stoichiometry; moisture; surface chemistry | Sieving; laser diffraction; BET (gas adsorption, Brunauer–Emmett–Teller); XPS (X-ray photoelectron spectroscopy); ICP-MS (inductively coupled plasma mass spectrometry) |
|  | Primary Shaping | Casting & molding | Pouring temperature; cooling rate; mold atmosphere; shrinkage | Gravity/die casting; injection molding; RTM (resin transfer molding) |
|  |  | Forming & extrusion | Extrusion temperature/pressure; draw ratio; strain | Rolling; forging; extrusion |
|  |  | Powder compaction | Compaction pressure; green density; density uniformity; binder content | Uniaxial pressing; CIP (cold isostatic pressing) |
|  | Consolidation | Sintering & densification | Sintering temperature/time; atmosphere; shrinkage; relative density | Conventional furnace sintering; controlled-atmosphere sintering; microwave sintering |
|  |  | Pressure-assisted consolidation | Temperature–pressure–time profile; densification rate; grain growth indicators | HP (hot pressing); HIP (hot isostatic pressing); SPS/FAST (spark plasma sintering/field-assisted sintering) |
|  |  | Melting & solidification | Solidification rate; thermal gradient; segregation index; superheat | Arc melting; induction melting; directional solidification; zone melting |
|  | Surface & Thin-film | Thermal & kinetic spraying | Coating thickness; porosity/density; bond strength indicators; deposition efficiency | Thermal spray (plasma/flame/cold); HVOF (high-velocity oxy-fuel) |
|  |  | Vapor deposition | Thickness; deposition rate; roughness; conformality | PVD (physical vapor deposition); sputtering; CVD (chemical vapor deposition); ALD (atomic layer deposition) |
|  |  | Surface modification | Modified layer thickness; roughness; chemistry; implantation dose/energy | Plasma treatment; ion implantation; laser surface processing; anodization |
|  | Additive Manufacturing | Layer-wise fabrication | Energy input; scan strategy; hatch spacing; build orientation | PBF (powder bed fusion); DED (directed energy deposition); FDM (fused deposition modeling); vat photopolymerization |
|  |  | Process stability | Porosity fraction; lack-of-fusion index; spatter/instability indicators; repeatability | In-situ optical/IR monitoring; melt pool monitoring; post-build XCT (X-ray computed tomography); SPC (statistical process control) |
|  | Joining & Assembly | Thermal & solid-state joining | Heat input; weld pool geometry; HAZ width; joint efficiency indicators | Arc/laser welding; brazing/soldering; friction stir welding; ultrasonic welding |
|  |  | Adhesive & hybrid joining | Cure cycle; bondline thickness; shear strength | Structural adhesive bonding; hybrid joints; mechanical fastening + adhesive |
|  | Nano-structuring | Bottom-up synthesis | Particle size distribution; shape anisotropy; yield; colloidal stability | Hydrothermal/solvothermal synthesis; chemical reduction; CVD growth; electrodeposition |
|  |  | Top-down structuring | Feature size; pattern fidelity; etch rate; damage/HAZ | Lithography; etching; FIB (focused ion beam); laser micromachining |
|  | Finishing & Circularity | Machining & finishing | Surface roughness; dimensional tolerance; burr/edge indicators | CNC machining (milling/turning/drilling); grinding; polishing; EDM (electrical discharge machining) |
|  |  | Recycling & recovery | Recovery efficiency; contamination level; recyclate morphology | Mechanical separation; solvent extraction; hydrometallurgy/pyrometallurgy (where applicable) |
| Design & discovery | Quantum & Atomistic | Electronic structure | Total/formation energy; band structure; DOS; work function | DFT (density functional theory); DFT+U; hybrid DFT |
|  |  | Atomistic dynamics | Diffusion coefficient; MSD; RDF; viscosity | MD (molecular dynamics); AIMD (ab initio molecular dynamics) |
|  |  | Defect & reaction kinetics | Defect formation energies; migration barriers; rate constants | Supercell defect calculations; NEB (nudged elastic band); transition-state search |
|  | Thermodynamics | Phase stability | Phase boundaries; phase fractions; stability regions; energy above hull | CALPHAD (calculation of phase diagrams); high-throughput DFT screening |
|  |  | Microstructure kinetics | Predicted size distributions vs time; coarsening rates; number density evolution | Precipitation/coarsening models; phase-field simulations |
|  | Continuum & Process | Multi-scale response | Stress–strain fields; residual stress; damage indicators | FEA (finite element analysis); CPFE (crystal plasticity finite element analysis) |
|  |  | Process–structure links | Thermal histories; cooling rates; predicted porosity risk; solidification metrics | Solidification modeling; thermo-mechanical process simulation; AM thermal models |
|  | Materials Informatics | Data curation | Dataset scope; schema/ontology mapping; provenance; versioning | ETL (Extract, Transform, Load) pipelines; metadata schema mapping; controlled vocabularies/ontologies |
|  |  | Machine learning | MAE (Mean Absolute Error)/RMSE (Root Mean Squared Error) /R²( Coefficient of Determination); prediction intervals; calibration error | Supervised ML (regression/classification); GNNs (graph neural networks); Bayesian methods |
|  |  | High-throughput discovery | Throughput; success/failure rate; candidate rankings; Pareto fronts | Automated workflows (HPC - High-Performance Computing); active learning/Bayesian optimization; multi-objective optimization |